## Slide 1: Pharmaceutical Related Gasket
Gasket Recommendations for the Pharmaceutical Industry

## Slide 2: PTFE Gaskets
Material of choice whenever low temperature flexibility or gasket memory is not required
Can remain in service for longer periods of time in both water and steam applications
Not recommended with large temperature variations due to creep and cold flow.
Operating temperature of -100ºF to 500ºF (-73ºC to 260ºC)

## Slide 3: Platinum Cured Silicone
Material of choice in sanitary pharmaceutical processes
Withstands temperature extremes
Resists product adhesion and maintains product integrity
Operating temperature of -40ºF to 450ºF (-40ºC to 232ºC)

## Slide 4: PTFE Envelope Gaskets
Envelope Type II
  Chemical resistance of PTFE and elastomeric insert of EPDM or FKM
  Available flanged and non flanged
  Meets FDA and USP Class VI standards

## Slide 5: Tuf-Steel®
New Standard in SIP (Steam in Place) gasket stability and longevity.
Composed of a unique 50/50 blend of PTFE and 316L atomized and passivated stainless steel
Unique blend provides outstanding performance in sanitary steam pipe connections with temperature ranges of -350º to 550ºF (-212ºC to 287ºC)
Also available in sheet

## Slide 6: Tuf-Flex® World’s Only Unitized Gasket
Combining the flexibility of an elastomer with the chemical resistance of PTFE
Performance with exceptional purity
  PTFE contact surface
  EPDM rubber inner core
Complete bonded construction provides flexibility in a high purity environment

## Slide 7: Ansi-Flex 150# Ansi Flange Gasket
PTFE unitized to an EPDM rubber inner core
  PTFE with mechanical characteristics and memory of elastomers
  Exceptional steam resistance, making it ideal for PVC and glass lined piping
  Outstanding performance under SIP/CIP conditions

## Slide 8: GYLON BIO-PRO®
No extrusion and cold flow
Temperature range of -346ºF to 500ºF (-210ºC to 260ºC)
High resistance to most chemicals & temperature cycles
Meets EN 1935/2004, USP Class VI, FDA-compliant and KTW approved

## Slide 9: GYLON® BIO-PRO PLUS™
Sealing integrity – proprietary GYLON® resists creep and cold flow
Temperature range of -450ºF to 500ºF (-268ºC to -260ºC)
Eliminates gasket recession and intrusion into the process flow
Ease of removal with zero gasket residue
Exceptional chemical and thermal cycling capabilities

## Slide 10: O-Rings, Quad Rings and Cord
Used in sanitary pipeline systems for pharmaceutical and bio-tech industries
Full product offering of AS568 dash numbers, metric and specialty o-ring sizes manufactured in EPDM, FKM, Buna, Silicone, Tuf-Steel® and Detectomer® Buna and FKM
Made using FDA or USP Class VI compliant compounds

## Slide 11: Smart Gasket®
Pharmaceutical in-line validation system
  Temporary or permanent use without custom installation
  Easy to expand
    1, 2, 3, and 4 internal ports available
Accessories are also available

## Slide 12: Biological Indicator
Self-contained indicator for sanitary process lines
Top loaded or inline positioning. Holds indicator in place for easy retrieval
Results within 24 hours

## Slide 13: Orifice Plates
Manufactured from 316L stainless steel
Drilled holes from 1/64” to 1 ½”
Vertical style is available
Tabs can be laser engraved to indicate orifice installation and hole size
Available in FKM, Silicone, EPDM, Buna, PTFE and Tuf-Steel®

## Slide 14: Gauge Guard Isolator Gaskets
Protects critical instrumentation with NO performance loss
Isolates hot or caustic saline solutions from instrumentation
Available in FKM, Silicone, EPDM, PTFE and Tuf-Steel®
Sizes include
  ½” & ¾” - .015 membrane thickness
  1”, 1 ½” & 2” - .010 membrane thickness

## Slide 15: Gauge Guard Protectors
Manufactured in Silicone and 316L stainless steel
Protects critical instrumentation while not in use

## Slide 16: Certificates
Every gasket comes with the applicable certifications
Buna is not ADI Free® (Animal Derived Ingredient Free)