## Slide 1: Gasket Basics
Useful Information on Elastomers, Gasket Anatomy and Making the Right Selection

## Slide 2: What is a Sanitary Gasket?
Sanitary Gaskets are used in the Food, Dairy, Beverage, Biotech, Pharmaceutical, and all other Sanitary Process industries to seal clamp connections in sanitary pipe lines.
Gets the name Tri-Clamp gasket from the Tri-Clover clamp used to hold the gasket in place

## Slide 3: Anatomy of a Failed Gasket

## Slide 4: Making a Gasket Selection

## Slide 5: Gasket Color Coding
Many sanitary elastomeric materials are the same in appearance. Rubber Fab sanitary gaskets are specifically color coded with dots to easily identify the gasket material.

## Slide 6: Rubber Fab Gasket Materials
Tuf-Steel® (PTFE and 316 Atomized Stainless Steel)
Tuf-Flex® (PTFE and EPDM)
PTFE
Platinum Cured Silicone
FKM Fluroelastomers
EPDM
Buna

## Slide 7: Buna Gaskets
The most versatile elastomer due to its resistance to many chemicals
Has good physical properties
Material of choice for food applications
Operating temperature of -30ºF to 200ºF

## Slide 8: EPDM Gaskets
Works well in both low and high temperatures
Good resistance to chemicals
Is peroxide cured
Operating temperature of -30ºF to 300ºF

## Slide 9: FKM Gaskets
Well suited for prolonged exposure to high operating temperatures
Good for steam applications
Operating temperature of -30ºF to 400ºF

## Slide 10: PTFE Gaskets
Material of choice whenever low temperature flexibility or gasket memory is not required
Can remain in service for longer periods of time in both water and steam applications
Not recommended with large temperature variations due to creep and cold flow.
Operating temperature of -100ºF to 500ºF

## Slide 11: Platinum Cured Silicone
Material of choice in sanitary water systems
Withstands temperature extremes
Resists product adhesion and maintains product integrity
Operating temperature of -40ºF to 450ºF

## Slide 12: Certificates
3-A Sanitary Standards
USP Class VI