## Slide 1: Food Related Gaskets
Gasket Recommendations for the Food Industry

## Slide 2: Buna Gaskets
The most versatile elastomer due to its resistance to many chemicals
Has good physical properties
Material of choice for food applications
Operating temperature of -30ºF to 200ºF (-34ºC to 93ºC)
Only elastomer that is not ADI® Free

## Slide 3: EPDM Gaskets
Works well in both low and high temperatures
Good resistance to chemicals
Is peroxide cured
Operating temperature of -30ºF to 300ºF (-34ºC to 149ºC)

## Slide 4: FKM Gaskets
Well suited for prolonged exposure to high operating temperatures
Good for steam applications
Operating temperature of -30ºF to 400ºF (-34ºC to 204ºC)

## Slide 5: Tuf-Steel®
New Standard in SIP (Steam in Place) gasket stability and longevity.
Composed of a unique 50/50 blend of PTFE and 316L atomized and passivated stainless steel
Provides outstanding performance in sanitary steam pipe connections with temperature ranges of -350º to 550ºF (-212ºC to 288ºC)
Also available in sheet

## Slide 6: Tuf-Flex® World’s Only Unitized Gasket
Combining the flexibility of an elastomer with the chemical resistance of PTFE
Performance with exceptional purity
  PTFE contact surface
  EPDM rubber inner core
Complete bonded construction provides flexibility in a high purity environment
Temperature range of -20ºF to 300ºF (-29ºC to 149ºC)

## Slide 7: Ansi-Flex 150# Ansi Flange Gasket
PTFE unitized to an EPDM rubber inner core
  PTFE with mechanical characteristics and memory of elastomers
  Exceptional steam resistance, making it ideal for PVC and glass lined piping
  Outstanding performance under SIP/CIP conditions

## Slide 8: Detectomer® Products
Full line of patented metal detectable/ x-ray inspectable elastomeric products
Helps to reduce product loss, product recalls and costly downtime
Available in Tuf-Steel®, Buna, Silicone, FKM and EPDM
Available in Tri-Clamp gaskets, sheet, screens, and o-rings

## Slide 9: Screen Gaskets
Provides particulate removal for almost all processing lines
Fluid conditioning seals designed to be interchangeable with standard sanitary clamp gaskets
Metallic screens are available in 316 stainless steel, in a variety of mesh sizes
Available in Buna, EPDM, Silicone, FKM, Tuf-Steel® and Detectomer®

## Slide 10: Certificates
Every gasket comes with the applicable certifications
Buna is not ADI Free® (Animal Derived Ingredient Free)